STANDARD OPERATING PROCEDURE FOR FORMING

- Relevant PPE’s such as hand gloves, safety helmets, and safety shoes are to be used.

- Identify the coil with sticker. Check coil width and thickness before loading.  If it is within specification as per the Supervisor’s instructions load the coil on pay off.

- Coil is then lifted with help of EOT crane.

- When coil is passed to mandrel, it has to be expanded and fix to the coil ID.

- Down the Snubber roll till it contacts to the coil.

- Binding strips are to be removed by binding cutter manually.

- Feed is given to the lead end of the sheet using pinch roll.

- Then the sheet is passes through loop pit table.

- Ensure that coil sheet enters through the entry guides/ pass before first pass.

- Coolant should be supplied as and when required from the coolant tank to the rollers.

- Observe profile dimensions, place intermediates guide wherever required.

- Check the profile dimensions and straightness before the profile enters cut-off tool and make necessary adjustment

- In case deviation persists inform superiors and make necessary corrections as per instructions.

- Adjust run off table as per the formed profile dimension.

- Adjust the length sensing device for the required length using encoder wheel.

- Cut the profile to the length adjusted and check all the dimensions of profile twist and bow with bow stand, for measuring camber use thread & for length use measuring tape

- If not Ok, make the necessary adjustments.

- If found Ok get clearance from shift In-charge and start production.

- While shearing the components check burr, bending if it is not ok then inform to shift incharge.

- Ensure use of gloves while removing the components from the run off table.

- Note down the profile dimensions in the mill report at regular intervals.

- For every 10 number of profiles, check the profile length.

- After forming sheet, the edges are grinded by hand grinding machine if required.

- Place the components in stacking order and bind using binding strip.

- If the component is of length more than 2 meters use lifting beam to lift with EOT crane to designated place.

SOP NO.: PIL/CRFS-PD-SOP-02 REV.00 DATE: 01.01.2022.