STANDARD OPERATING PROCEDURE FOR SEMI CONTINUOUS PICKLING

BOILER OPERATION REQUIREMENT

- Start the boiler and maintain the steam pressure between 4 to 8.5 kg/mm square.

Open the main steam valve for releasing the steam for heating the acid / rinse water and as well as hot air blower.

UNCOILER DESK OPERATION

- Identify the coil with sticker/Coil part no. as per programme.

- Transfer the coil from HR slitter or stock yard to SCP bay.

- Put the coil on the coil car with the help of EOT crane.

- Bring the coil towards the mandrel

- Feed the coil into mandrel till the proper grip is made

- Adjust the center line of the coil by shifting the un coiler mandrel base.

- Lower the snubber roll and cut the binding strip

- Feed the strip by last part and join the both ends by lap welding

- Into the pinch roll and leveler and to take the strip, simultaneously adjust the guides

- Jog the coil in forward direction to enter into the pinch roll and leveler.

- Adjust the peeler table raising or lowering and moving in out depending on the diameter of the coil.

- Lower the pinch roll leveler and jog the strip

- Check the lead end of the strip, if it is bad cut the strip.

- Check the proxies at i. Peeler table, ii. Snubber, iii. weld clamps

- Thread the line toward the re coiler and observe the strip as it passes through

  - Process tanks I,II &III

  - water rinse tanks I,II &III

The following acid concentrations and % of iron to be maintained in the acid tank

Acid Tank I II III

Concentration 2-7 6-14 9-18%

% Iron content 22 max 22 max 20 max

Temperatures 450-600 500-650 550-700

- Switch on the air drier line valve. Run the line till the joint reaches to coil area .

- Ensure the peeler table and re-winder mandrel gripper in position to receive the strip.

- Adjust the side guides and jog the strip till it reaches the mandrel.

- Expand the mandrel after gripping the strip, and lower the peeler table to original position.

- Jog the strip slowly and wind the re-coiler drum till one wrap develops over it.

- Switch on the emulsion oil application to the strip

- Switch on line, run and slowly raise the speed of the strip, observe pickling surface quality, if quality is correct continue with the same speed otherwise reduce the speed until quality is attained and maintain the revised speed.

- Now the re-coiler operator will run the line strip till the winding is completed and stop oil application.

- Put a binding strap around the coil, give identification with coil card/ sticker and sent to next work center.

- Write the production report.

SOP NO.: PIL/11MFG/PM/07 REV.00 DATE: 01.10.2021