WORK INSTRUCTIONS FOR MIG (METAL INERT GAS) WELDING

- Recommend PPEs to be used.

- Only qualified welder has to proceed the following instructions given below

- Check manual running of the machine i.e. rotate the coil by operating the torch to check the coil feed rate.

- Check the electrical cables of the machine, collect the job drawing from the production in-charge and check the availability gas cylinder (CO2-18%, Argon-82%).

- Clean the surface with brush to remove the dust and ensure surface is rust free.

- By EOT crane load the fabricated jobs to the required position on the table/fixer.

- Select the electrode, contact tip and nozzle required and fit in the welding torch.

- Switch ON the main power supply

- Adjust the current and voltage as per the instructions

- Start the machine and set the required speed and feed manually

- After completing the root run check defects like blow holes, under cuts etc.

- Complete the welding for the required weld thickness as per drawing.

- Clean the area from welding internals and clean the welding M/C properly and the cable is proper way.

SOP NO.: PIL/55FAB/PROD/PM/D08 REV.00 DATE: 27.08.2021