STANDARD OPERATING PROCEDURE FOR FLUX BAKING AND HOLDING

- Purpose: To provide guidelines for easy process for Flux Baking

- Scope: This procedure is applicable to applicable to Flux Baking

- Responsibility:

Head Production, Concern Engineers and the Shift In - Charge along with their Operators and the Sub - Contractors are responsible for this activity.

- Procedure

  - Operator shall fill the Flux in Flux Tray of Baking Oven whenever required.

  - Check the unit is working properly and temperature to be " SET " at 2500 Celsius.

  - For " TWO HOURS " Flux to be heated at 2500 Celsius temperature.

  - After " TWO HOURS " Flux to be transfer in Holding Oven for Holding the temperature of 1000 Celsius up to Flux uses.

*** Temperature and time shall meet the flux manufacturer recommendation

  - Operator shall issue the Flux to Saw Welder from Holding Oven.

  - Operator shall update Flux Baking Register which indicates: -

  - Baking Temperature, Flux in Time, Out Time, Holding Temperature,

  - Ensure proper electrical connections with the work piece and ensure good ground.

  - Ensuring the unit is working and in good condition.

  - Keep the required quantity of the Flux and Electrodes inside the unit that are to be used for a da

  - Adjust the appropriate temperature as and when required.

  - Ensure all the electrical cables are intact and are not damaged.

  - Maintain the machine in good working condition. He keeps his working area clean.

  - In case of breakdown of the machine he informs his supervisors who in turn advices the plant maintenance department through the breakdown slip.

  - Operator is responsible for " Safety Practices " at the time of work.

  - Use of helmets, safety shoes, goggles and hand gloves is compulsory.

  - At the time of flux taking from oven, oven should be " OFF ".

  - DO NOT use TORN hand gloves.

  - DO NOT touch the flux with bare hand and ensure that hand gloves are worn.

  - DO NOT touch the coil which is inside the oven.

  - DO NOT touch any electrical cable near the panel.

SOP NO.: PTC/Fab/PROD/ REV.00