SAFE OPERATING PROCEDURE FOR WELD REPAIR

- Purpose: To provide guidelines for easy process for Weld Repair.

- Scope: This procedure is applicable to Weld Repair.

- Responsibility:  Head Production / Fabrication, Concern Engineers and Shift In - Charge along with their operators are responsible for this activity.

- Procedure:

- Place the steel backing strip at one of the depth of hole and either tack [or] seal welds around the backing strip.

- Gouge a ‘U’ shaped cavity down to the backing and fill the cavity by welding using a stringer bead technique.

- After the first side is welded, gouge another side to make an " U " shaped cavity completely removing the temporary backing and complete by welding using a stringer bead technique.

- The backing strip material shall have similar composition of base metal.

- Ensure adequate ventilation to remove welding fumes.

- Clear the work area of flammable materials and have fire extinguishing equipment readily available.

- Properly ground the welding equipment to prevent electrical shock

- Use of helmets, hand gloves, goggles and safety shoes is compulsory.

- Proper care must be taken while working / inspecting under overhead cranes.

SOP NO.: PTC/Fab/PROD/ REV.00